## Slide 1
WASHING OF HIGH GRADE INDIAN NON-COKING COAL FOR STEEL MAKING IN BLAST FURNACE ROUTE
PRESENTED BY
GAUTAM SENAPATI
AVP ( washeries), coal business, JSW Steel

## Slide 2: BACK GROUND
AS PER NATIONAL STEEL POLICY, GOI HAS TARGETED TO PRODUCE 300 MTPA CRUDE STEEL BY 2030
ABOVE 60% STEEL PRODUCTION IS EXPECTED TO BE THROUGH BF ROUTE, IN WHICH COKING COAL IS THE KEY INPUT RAW MATERIAL.
HARDLY 10% OF THE COAL RESEVE IN INDIA IS COKING COAL.
INDIAN COKING COAL IS GENERALLY CHARACTERIZED BY HIGH ASH CONTENT AND DIFFICULT TO WASH. HENCE, ONLY APPROX. 20% OF THE RAW COKING PRODUCED IN THE COUNTRY IS CONSUMED IN STEEL SECTOR.
ALL INTEGRATED STEEL MAKERS IN BF ROUTE ARE DEPENDENT ON LOW ASH IMPORTED COAL ( BOTH COKING & NON-COKING COAL) FOR PRODUCTION OF STEEL
PRODUCTION OF COKING COAL BELOW 10% ASH FROM INDIAN COAL AS REQUIRED IN BF ROUTE IS PRACTICALLY NOT POSSIBLE.
OPPORTUNITY EXISTS IN WASHING HIGH GRADE NON-COKING COAL FOR PRODUCTION OF LOW ASH NON-COKING CLEAN COAL FOR STEEL MAKING IN BF ROUTE.

## Slide 3: Import of various types of coal
COAL TYPE | Fy 2022-23 ( MT) | Fy 2021-22 ( MT) | Growth%
COKING COAL | 54.46 | 51.65 | 5.44
PCI COAL | 15.69 | 13.66 | 14.87
NON-COKING COAL | 162.04 | 124.99 | 29.88
Ref : coal Insight |  |  | 

## Slide 4: USE OF NON-COKING COAL IN STEEL MAKING
PCI
BLEND WITH COKING COAL IN STAMP CHARGING BATTERY
COREX
DRI
USE OF NON-COKING COAL IN JSW STEEL:
PCI : Approx. 200 KG/ TON HOT METAL
NON-COKING COAL USAGE IN JSW COAL BLEND: Approx. @9% WITH IMPORTED COAL.
BUT ENTIRE NON-COKING COAL CONSUMED IN JSW IS IMPORTED.

## Slide 5: BRIEF ABOUT STEEL MAKING IN JSW STEEL
PRESENT CRUDE STEEL PRODUCTION CAPACITY : 27.7 MTPA
PLANNED TO BE EXPANDED TO : 37 MTPA BY 2024-25
JSW VIJAYNAGAR STEEL PLANT, BELLARY, KARNATAKA
DOLVI STEEL PLANT, MAHARASTRA
BHUSHAN POWER AND STEEL LTD, SAMBALPUR, ODISHA
MONNET ISPAT LTD, RAIGAD, CHHATRISGARH
SALEM STEEL

## Slide 6: TECHNOLOGY OF STEEL MAKING IN JSW
VIJAYNAGAR STEEL, BELLLARY, KARNATAKA
  HIGH CAPACITY BLAST FUNACE ( ABOVE 4000 CBM)
  COREX TECHNOLOGY.
  DOLVI STEEL PLANT, MAHARSTRA
  HIGH CAPACITY BLAST FURNACE ( ABOVE 5000 CBM)
  BHUSHAN POWER AND STEEL LTD.
  SMALL CAPACITY BLAST FURNACE ( 1000/2000 CBM)
  DRI PROCESS
  MONNET ISPAT, RAIGAD, CHHATRISGARH
  DRI PROCESS
  JSW, SALEM
  SMALL CAPACITY BLAST FURNACE
  COKE MAKING TECHNOLOGY : STAMP CHARGING BATTERIES

## Slide 7: COAL CONSUMPTION IN JSW STEEL
JSW IS PRESENTLY FULLY DEPENDENT ON IMPORT OF COAL ( BOTH COKING AND NON-COKING )
COKING COAL : 13-14 MTPA
NON-COKING COAL IN BF ROUTE ( PCI & stamp charging battery) : 5-6 MTPA

## Slide 8: BROAD QUALITY SPECIFICATION OF NON-COKING COAL FOR USE IN STEEL MAKING IN BF ROUTE
QUALITY PARAMETER | PCI | COREX/ stamp charging battery
ASH% | <10% | < 10%
GCV | Above 7000 | Above 7000
VM% | 15-20% | < 30%
FC% | Above 70% | Above 60%
ASH FUSION TEMP | 1250- 1500 deg C | 1300- 1500 deg C
HGI | Above 70 | -
ALKALI% | Less than 2% | Less than 2%
IM% | <= 2% | <= 2%
S% | Less than 0.6% | Less than 0.6%
P% | Less than .05% | Less than .05%
CSN | ~1 | ~1

## Slide 9: WASHING OF HIGH GRADE NON-COKING COAL FOR USE IN STEEL MAKING- WHY ?
To reduce ash content in washed non-coking coal below 10%
Steel making requires consistent quality.
Stringent quality parameter of coal as required in steel making in BF route.
Washing not only reduces ash content in washed coal but also improves other parameters, like, VM%, GCV, CSN etc.
Non-coking coal which can be beneficiated:
Preferably above G6 grade
Conducted washability study of G4 grade ECL coal and found to be feasible.
Reserve above G6 grade : More than 35 BT
Present production above G6 grade : Approx. 30 MTPA

## Slide 10: POLICY SUPPORT AS REQUIRED FOR INCREASE IN USE OF NON-COKING COAL IN STEEL MAKING IN BF ROUTE
Except GCV and ash parameter, no other quality parameter data is available with respect to non-coking coal in public domain.
Detailed coal characterization data is required by the steel maker with respect to non-coking coal, before considering the use.
Extensive source specific washability study needs to be done.
Support with respect to sampling and analysis including pilot level testing for use of non-coking coal in steel making.

## Slide 11
THANK YOU